DINO
180° DOUBLE BEARING HINGE

SPECIFICATIONS

The hinge shall be 100% mechanical (no electronic components).

The hinge shall be available in either a black or silver color.

PERFORMANCE

The hinge shall be specifically made for outdoor use (IP69).

The hinge shall be maintenance free (no greasing nor oil refill).

The manufacturer warranty shall be 3 years.

INSTALLATION

The hinge shall have pre-mounted fasteners (no welding) with stainless steel bolts. 
All brackets for fixation should come with the product.

The same hinge shall be able to be used for both left and right turning gates.

MATERIAL

The mechanism shall be made out stainless steel and aluminum components.

The housing of the mechanism shall be made from extruded, powder coated aluminum 
(no wet painting or anodization). The powder coating shall be according to the Qualicoat standards.

The hinge shall have a corrosion resistance of 500h salt spray according to ISO9227.

The hinge shall be fully weather- and dustproof.

The hinge shall have a UV-resistance against discoloration of 500h.